Journal of Zhejiang University-SCIENCE A   in press
www.jzus.zju.edu.cn; www.springer.com/journal/11582
E-mail: jzus_a@zju.edu.cn
6
|  J Zhejiang Univ-Sci A   in press
7
J Zhejiang Univ-Sci A   in press  |

[image: image1.wmf]=,

E

s

e

Research Article
https://doi.org/10.1631/jzus.A2600xxx
An adaptive design method for understanding tolerance in the precision stamping process
San ZHANG1,2, Sisi LI1(, Zhiwu WANG3
1MOE Key Laboratory of XXXX XXXXX, Zhejiang University, Hangzhou 310027, China
2Shanghai XXX XXXX XXXX Co. Ltd., Shanghai 201100, China
3Department of XXXX XXX, University of XXXX, Liverpool, L69 7ZX, UK

Abstract: With the development of precision manufacturing, the understanding of tolerance has become a research hotspot in the field of manufacturing. An adaptable design method for understanding tolerance in the precision stamping process is proposed in this study. First, fluctuations of tolerance which are caused by differences in the stamping process are analyzed, such as differences in material and thickness, which can lead to changes in the metal flow stress curve. Second, a condition-driven adaptive design method is constructed based on a monitoring system and hydraulic control system. The mapping rules between multiple disturbance factors and the execution strategy are established by the hidden Markov model algorithm. Third, executive parameters, such as velocity, pressure, and gaps, are calculated and optimized by the data statistics of partial tolerance fluctuations in the control module. Then disturbances of various conditions could be adaptively controlled timely and effectively by the executive parameters. Finally, the adaptive design method for tolerance of one precision stamping part is applied, and the effect of the application is proved by the optimized results. 

Key words: Adaptive design; Tolerance; Condition-driven; Precision stamping process
1  Introduction

Authors who submit their manuscripts (for JZUS-A, in Word format only) should follow the formats according to this sample. These are formats for authors typesetting for Journal of Zhejiang University-SCIENCE A (JZUS-A). This document has been prepared using the required format. The paper is to be written in two-column format and be right and left justified. Please try to use the paragraph styles contained in this document.
Figures must be numbered consecutively with Arabic numerals, and each figure must be placed in the text following the paragraph in which it is first mentioned. A caption giving the figure number and a brief description must be included. The caption should be understandable without reference to the text. Figures should be cited in the text using the following format: Fig. 1, Fig. 1a, Figs. 1 and 2, Figs. 1–3, or Figs. 1a–1c.
There will be an extra charge for those graphics considered for publication in color. Authors are expected to use different line types to distinguish the different parts of a figure that they do not want to have published in color.
[image: image20.png]


As society advances, product quality requirements are continuously improved in the marketplace. Manufacturing enterprises are facing increasing cost and technical pressures in the production of precision parts. High quality parts, which with high dimensional accuracy, smooth blanked surfaces, and good interchangeability, can be obtained through precision stamping technology processing. Some subsequent processing operations can be reduced or even cancelled, such as leveling and grinding. Product quality and production efficiency can be improved by precision stamping processes at a relatively low cost. In industrialized countries, precision stamping technology is becoming more widely applied in various industrial sectors including automobile manufacturing (Weng and Xu, 2012).
As technology advances, many researchers have made a lot of achievements in the field of dimensional tolerances design and control. Requicha (1983) proposed an offsetting tolerance zone theory, which laid the theoretical basis for computer-aided tolerance design. Virtual boundary requirements (VBR) were proposed to restrict the maximum physical condition and the smallest entity state of the parts, and then tolerance specification language was used to describe the VBR model (Etesami, 1993). The computer-aided tolerance optimal design method was proposed by using the simplified integrating region and Monte Carlo simulation (Wu and Yang, 1999). The robust tolerance design method was studied for manufacturing (Cao, 2003). A new functional tolerancing method was presented for a geometrical functional requirement to geometrical specification (Yang et al., 2010). Meanwhile, some other research related to computer-aided tolerance design were being proposed, such as sequential tolerance control (STC) (Fraticelli et al., 1997, 1999), some extension applications of sequential tolerance control (Cavalier and Lehtihet, 2000), a low-cost fault tolerance approach (Vakili et al., 2009), material selection strategy for optimal structural design (Qiu et al., 2013), and a multi-physics coupling field finite element analysis (Zhao et al., 2009).
2  Tolerance fluctuation analyses

2.1  Txxxx xxxx xxxxx
Precision parts are produced based on geometric dimensions and process routes determined during detailed design. Aiming for high quality, operators process the raw material into parts using equipment in the production environment. There are inevitable disturbance factors (such as man, material, machine, method, measure, and environment (5M1E)) in the production environment affecting the processing quality. Tolerance fluctuations are caused by 5M1E in the manufacturing process which results in a loss of quality. Tolerance fluctuations would cause geometry errors of the precision parts in the manufacturing process, while there will also be dimension and position errors. The form and position errors impact the performance of the parts (assembly, structural strength, contact stiffness, interchangeability, sealing, motion accuracy, and meshing, etc.) in varying degrees. 
When the load stress is less than the proof stress, the strain ε is proportional to the stress (. The final value of the strain is determined by the modulus of elasticity and obeys Hooke’s law:


[image: image21.png]JZUS




                                   (1)
where E is a constant.

When the load stress exceeds the proof stress, metallic materials begin to flow. The required stress can be obtained by the Hall-Petch formula:


[image: image2.wmf]eiycvoy

,

Rkd

ssss

=+D+D+D+

         (2)
where Re is the elastic limit, the load stress when the metal begins to flow; (iy is the Peierls stress, the internal friction which must be overcome when the metal flows; Δ(c is the increment of strength of materials caused by the solid solution intensification; Δ(v is the increment of strength of the materials caused by strain hardening; Δ(o is the increment of strength of materials caused by dispersion strengthening;  
[image: image3.wmf]y

kd

 is the increment of strength of the materials caused by fine-grain strengthening; ky, the resistance of the grain boundary, is constant; and d is the diameter of the grain. Eq. (2) shows that the elastic limit of the metal material is the superposition of the values of different mechanisms. These values constitute the material strength. 
Fig. 1 is the schematic diagram of the plastic deformation of metallic materials in the precision stamping testing process. 

[image: image4.png]I I

Blanking surface e .
_ | Modification |
distance | extension I
2B - -

ETﬁx__

/177777,
/





Fig. 1  Plastic deformation of metallic materials
Stamping trials were conducted using two types of steel materials (Q345 and 35#) to study the hardening state. The measurement data were carried out by quadratic fit. Figs. 2 and 3 were obtained to show stress variation in the steel. 
[image: image5.png]Thickness of material (mm)

A
—
I

10 | A e Distance from surface
A 1.0 mm
9 | A ® 0.5 mm
LO ¢ 0.3 mm
gl = = 0.2 mm
. N * 0.1 mm
7 g
6| 2
9
51 8
m
4 |
3 |
2 |
1 |
O — —r »— | |
150 200 250 300 350 400

Stiffness HV 0.2




Fig. 2  Hardening state curves of Q345
[image: image6.png]Thickness of material (mm)

g I
7 L
6
Distance from surface

5t i A 1.0 mm

N © 0.5 mm
4| CCD ¢ 0.3 mm

5 = 0.2 mm

‘5 0.1 mm
3t 2

O
2L ®©

M
1|
0 * / '
150 200 250

Stiffness HV 0.2

300




Fig. 3  Hardening state curves of 35#
2.2  Txxxxx xxxx xxxxx
The fitting curve of the experimental data is shown in Fig 2. The test object was a generic steel material (No. Q345). The average curvatures of the hardening state curves of the material forming were different with different distances to the precision stamping surface when the load stress exceeded the proof stress. The smaller the distance, the greater the material hardening change. The hardening degree of distance 0.1 mm was greater than 1 mm (Fig. 2). The same situation happens in Fig. 3 with the test object No. 35#. The basic strength of the material stayed the same when the load stress was less than the proof stress or the distance was more than 1 mm. 

By analyzing the results shown in Figs. 2 and 3, we can see that the hardening state curves of different materials were different. Under the same distance, the values of the hardening state of different materials were different. Stiffness presents the physical parameter of pressure in the stamping process. Oriented to different raw materials, thickness, and molds, fluctuations of geometric tolerance were caused and the processing quality decreased without the adaptive design for the pressure control. 

3  Adaptive design model
The precision stamping device is constituted by the function, behavior, structure, carriers, and other design elements. In the mechanical system design theory, there are reciprocating mapping relationships among function domain (F-domain), behavior domain (B-domain), and carrier domain (C-domain) (Umeda et al., 1990). Functionality is achieved by the combination of product behavior. Behavior is performed by the carriers. The carrier is the basis of components that make up the complete device. During the precision stamping process, the device performance degrades because of condition fluctuations.

The state data are traced back to the source of the fluctuations in condition factors by the hidden Markov model (HMM). The carrier domain is calculated through the mapping relationships of the device structure. Feedback of the tolerance fluctuations is regulated by controlling the execution parameters of the carrier. Then a closed-loop feedback adaptive control system for computer-aided tolerance can be proposed.

The HMM is expressed by the following five parameters (Rabiner, 1989):
N: The number of hidden states (θi) of the hidden Markov chain is expressed as N, and the states are expressed as S. The state of the hidden Markov chain at time t is expressed as qt.


[image: image7.wmf]{

}

{

}

12

12

,,,,

,,,.

N

tN

S

q

qqq

qqq

=

Î

L

L

                         (3)
M: The number of different values monitored by the corresponding sensors in the process is expressed as M. The set of monitoring values is represented as V, and vi is the element of the set V. 
The monitoring value at time t is expressed as ot.


[image: image8.wmf]{

}

12

,,,.

tM

o

nnn

Î

L

                        (4)
π: The probability distribution of the initial state (qt) in the process is expressed as π.


[image: image9.wmf]{

}

12

,,,.

N

π

π

π

π

=

L

                        (5)
Supplementary, πi=P(q1=θi) and 1≤i≤N.

A: The state transition probability matrix is expressed as A.

[image: image10.wmf](),

´

=

ijNN

a

A

                             (6)

[image: image11.wmf]1

()

ii

π

Pq

q

==

 and 1≤i≤N, 1≤j≤N.
B: The monitor value probability matrix is expressed as B.
The states of tolerance fluctuations are identified by the following three steps:

Step 1: Initial values selection. Statistical data of the tolerance fluctuations in the precision stamping process are analyzed. The initial values of A and B are selected in the historical statistics to meet the constraints of Eqs. (3)–(6). 
Step 2: Model training. The probability is defined as ξt(i, j) when HMM is in state θi at time t, while in state θj at time t+1 based on the given training sequence O and model λ. 

The probability of Markov chain in the state θi at time t is expressed as γt(i):


[image: image12.wmf][

]

1

()()

()(,).

()

N

tt

t

j

aibi

iij

PO

gx

l

=

==

å

                (7)
Parameters are conducted by several iterative operations by using the revaluation formula of the Baum-Welch algorithm. Convergent parameters of the model 
[image: image13.wmf](,,)

π

=

%%

%

%

l

AB

 were obtained to meet the requirements of the error range.

Step 3: State solution. State sequence Θ is estimated by the Viterbi algorithm in those cases when the value of P(Θ|V) is at the maximum. It can be calculated by the Bayes formula.
The following formula can be obtained after transformation:

[image: image14.wmf]1

1

21

()()()()()=

()().

Θ

nn

tttt

tt

gV=P

Θ

PV

Θ

PPV

Θ

PPv

q

qqq

-

==

=

ÕÕ

          (8)
The model parameters of HMM are obtained by revaluating the monitoring data. The maximum values of the sub-state are calculated for each state at each time. The sequence Θ of the state values at each time can be obtained by accumulating the sub-state values. The sequence is the hidden tolerance fluctuant states in the precision stamping process.

Once the volatility of the tolerance fluctuations exceeded the tolerance range in design, the adaptive control strategy would be activated in the computer numerical control system. The process execution parameters were adjusted adaptively to reduce the volatility.
4  Results and discussion
A precision stamping process is used to cut or mold materials based on the plastic shear theory, and it is pressed on a dedicated piece of press equipment using a precision die with a non-traditional structure. The precision stamping process makes the materials to generate the plastic deviatoric deformation under huge pressure. The adaptive design method is proposed to control the process parameters which would reduce the tolerance fluctuations. It is a very significant approach for improving the processing quality and accuracy in the precision stamping process. Fig. 4 is a design model of a dedicated die in the precision stamping process.

[image: image15.emf]F

x

F

y

F

z


Fig. 4  Design model of dedicated die
Precision stamping tests were carried out several times under the traditional processing methods on steel materials (No. 35#). The test data is shown in Table 1.

Basic process parameters were held constant, while some particular condition factors were allowed to fluctuate in the trials. It was shown that the volatility of the tolerance fluctuation was different in different trials. Comparing three sets of data from trials S1, S2, and S3, the tolerance changes by 0.070, 0.035, and 0.024, respectively. The fluctuation range is about 0.028. By analyzing the trials S2, S4, and S5, the fluctuation range is about 0.270. The amount of the fluctuation range for this data set is 10 times that of the former. The fluctuation range should be reduced by redesigning the process parameters when the condition factors change. 

Process parameters were adjusted adaptively under the adaptive method by the monitoring system and HMM algorithm in five different types of tests. The simulations of the adaptive process parameters are shown in Figs. 5–7. The results of the adaptive control method of tolerance in the precision stamping process are shown in Table 2.
The XXXXX is given in Section S1 and/or Table S1 of the electronic supplementary materials (ESM), including the solution steps of the XXXX.
Table 1  Measured data of the experiments in five states

	Trial
	Blanking clearance (mm)
	Radius of punch (mm)
	Radius of die (mm)
	Fillet radius of die (mm)
	Thickness of steel (mm)
	Velocity (mm/s)
	Metal type 
	Pressure 
(×104 N)
	Displacement (mm)
	Angle (°)

	S1
	0.05
	9.95
	10
	0.1
	1.0
	20
	35#
	2
	0.260
	0.70

	S2
	0.10
	9.90
	10
	0.1
	1.0
	20
	35#
	2
	0.292
	0.35

	S3
	0.15
	9.85
	10
	0.1
	1.0
	20
	35#
	2
	0.326
	0.24

	S4
	0.10
	9.90
	10
	0.1
	1.5
	20
	35#
	2
	0.375
	0.97

	S5
	0.10
	9.90
	10
	0.1
	2.0
	20
	35#
	2
	0.498
	3.05


[image: image16.png]21600+

17300}

12900

Load (N)

8630 |

4320 |

0 00693 0.1390 02080 02770 0.3460
Stroke (mm)




Fig. 5  Simulation of adaptive control in S1
[image: image17.png]O . . . . .
0 0.0687 0.1370 0.2060 0.2750 0.3450
Stroke (mm)




Fig. 6  Simulation of adaptive control in S2
[image: image18.png]20700 |
16600 |
Z 12400 |
e
©
S 8280¢

4140 |

0 . . . . S
0 0.0736 0.1470 0.2210 0.2940 0.3680
Stroke (mm)




Fig. 7  Simulation of adaptive control in S3
Table 2  Measured data of the experiments in five states

	Trial 
	Max 
pressure (×104 N)
	Displacement (mm)
	Distance 
of fracture (mm)
	Tolerance fluctuation (mm)

	S1
	2.04
	0.235
	0.248
	0.013

	S2
	2.01
	0.262
	0.281
	0.019

	S3
	1.96
	0.296
	0.318
	0.022

	S4
	2.01
	0.345
	0.362
	0.027

	S5
	2.93
	0.398
	0.434
	0.036


The relationships among the stamping pressure, breakpoints, and the displacement of the punch were obtained by fitting curves in Matlab. The results can be seen in Figs. 5–7. As the blanking clearance increased (as trials S1, S2, and S3), the displacement of the punch increased non-linearly (0.235, 0.262, and 0.296), and the maximum stamping pressure decreased (2.04, 2.01, and 1.96). The fluctuation range is about 0.009. As shown, the thickness of the steel changed (as trials S2, S4, and S5), the distance of the fracture increased (0.281, 0.362, and 0.434), and the maximum stamping pressure increased (2.01, 2.01, and 2.93). The fluctuation range is about 0.017. Compared with the fluctuation range 0.270, the fluctuation range was significantly reduced (from 0.270 to 0.017, turned around 1/16). The process quality was significantly improved by using the adaptive design method. 

5  Conclusions

An adaptive design method to the tolerance fluctuation problem in machining of precision parts has been developed and presented. Status and trends of tolerance fluctuations of parts are calculated by the HMM based on the monitoring data of the press equipment. There are some meaningful observations in this study which are presented as follows:
1. Stamping experiments were conducted in two kinds of steel materials (Q345 and 35#) to study the parameter sensitivity around the distance of the molds or thickness of materials and stiffness.

2. The sequence of the hidden tolerance fluctuant states in the precision stamping process at each time can be obtained by using the HMM algorithm. 

3. The adaptive design of the tolerance fluctuations is simulated and analyzed by the precision stamping process through controlling the process parameters, such as pressure of the hydraulic press, displacement of molds, distance of the fracture in materials, and so on.

Several other benefits are foreseen using this method and are actively being investigated. These include: coupling stress of the disturbance factors which fluctuates the tolerance, the generic mechanism which causes the tolerance, the comprehensive program which restricts the form and position errors in the tolerance range.
Acknowledgments

This work is supported by the National Natural Science Foundation of China (Nos. 00000001 and 00000002), the National Key Research and Development Program of China (No. 2000000001), the Zhejiang Provincial Natural Science Foundation of China (No. LR200000000), and the Innovation Foundation of the State Key Laboratory of Fluid Power Transmission and Control, Zhejiang University, China. We thank Dr. Liu ZHAO (College of XXXX, Zhejiang University, China) for xxxxx xxxx.

Author contributions
XXX designed the research. XXXX and XXX processed the corresponding data. XXX wrote the first draft of the manuscript. XXXXX helped to organize the manuscript. XXXX revised and edited the final version. 

Conflict of interest 

San ZHANG, Sisi LI, and Zhiwu WANG declare that they have no conflict of interest.
Declaration on the use of generative AI tools
As generative AI tools have become increasingly popular, authors must declare whether they have used these tools during the preparation of the manuscript.
Data availability 

The data that support the findings of this study are available from the corresponding author upon reasonable request.

References
Cao YL, 2003. Study on the Methodology and Technology of Robust Tolerance Design for Manufacture. PhD Thesis, Zhejiang University, Hangzhou, China (in Chinese).

Cavalier T, Lehtihet A, 2000. A comparative evaluation of sequential set point adjustment procedures for tolerance control. International Journal of Production Research, 38(8):1769-1777. 

https://doi.org/10.1080/002075400188582
Etesami FA, 1993. A mathematical model for geometric tolerances. Journal of Mechanical Design, 115(1):81-86. 

https://doi.org/10.1115/1.2919329

Gorini S, Quirini M, Menciassi A, et al., 2006. A novel SMA-based actuator for a legged endoscopic capsule. First IEEE/RAS-EMBS International Conference on Biomedical Robotics and Biomechatronics, p.443-449.

https://doi.org/10.1109/BIOROB.2006.1639128

ISO (International Organization for Standardization), 1982. Steels-Classification-Part 1: Classification of Steels into Unalloyed and Alloy Steels Based on Chemical Composition, ISO 4948-1:1982. ISO, Geneva, Switzerland.

SEPA (State Environmental Protection Administration), 1997. Integrated Emission Standard of Air Pollutants, GB 16297-1996. National Standards of the People’s Republic of China. 
Sweeney L, 2000. Uniqueness of Simple Demographics in the U.S. Population. Technical Report No. LIDAP-WP4, Laboratory for International Data Privacy, Carnegie Mellon University, Pittsburgh, USA.
Tanner NA, Wait JR, Farrar CR, et al., 2003. Structural health monitoring using modular wireless sensors. Journal of Intelligent Material Systems and Structures, 14(1):43-56.

https://doi.org/10.1177/1045389X03014001005

Wu ZT, Yang JX, 1999. Computer Aided Tolerance Optimization Design. Zhejiang University Press, Hangzhou, China, p.85-124 (in Chinese).
Electronic supplementary materials
Section S1, Table S1, Figs. S1–S3
中文概要（请作者提供）
题目：面向认知公差的精密冲压工艺适应性设计方法
作者：张三1,2，李四四1，王之五3
机构：1浙江大学，XXXX教育部重点实验室，中国杭州，310027；2上海XXX有限责任公司，中国上海，201100；3利物浦大学，XXXX学院/系，英国利物浦，L69 7ZX
目的：精密冲压工艺过程中环境变量的波动导致工件出现破裂和皱褶等缺陷。本文旨在探讨精密冲压工艺过程中环境变量（工件材质、冲压速度、压力和温度变化等）对冲压质量的影响，研究适应性工艺设计方法，以提高精密冲压工件的质量。

创新点：1. 通过马尔科夫模型方程，推导出环境变量与精密加工波动公差之间的关系；2. 建立试验模型，成功模拟适应性冲压工艺过程。
方法：1. 通过实验分析，推导出冲压过程中的晶粒流动和强度变化对成型零件的尺寸公差波动产生较大的影响（图2和3）；2. 通过理论推导，构建环境变量与加工波动公差之间的关系，得到适应性的工艺参数调节方案（公式(6)）；3. 通过仿真模拟，运用适应性设计方法在精密冲压过程中对工艺参数进行适应性调节，验证所提方法的可行性和有效性（图5）。

结论：1. 精密冲压过程中工艺参数需要根据不同的环境变量进行调节；2. 环境变量与加工波动公差之间存在映射关系，运用隐马尔科夫模型实现关联表征；3. 运用适应性设计方法对精密冲压工艺参数进行调节，加工波动公差明显减小，工件质量得到提高。
关键词：适应性设计；公差；工况驱动；精密冲压工艺
===========================================
参考文献格式要求(Reference format):

（点击可下载本刊Download网站上对应的Endnote模板）
期刊论文(Journal article)
Tanner NA, Wait JR, Farrar CR, et al., 2003. Structural health monitoring using modular wireless sensors. Journal of Intelligent Material Systems and Structures, 14(1):43-56.

https://doi.org/10.1177/1045389X03014001005
会议文章(Conference)
Gorini S, Quirini M, Menciassi A, et al., 2006. A novel SMA-based actuator for a legged endoscopic capsule. First IEEE/RAS-EMBS International Conference on Biomedical Robotics and Biomechatronics, p.443-449.

https://doi.org/10.1109/BIOROB.2006.1639128

专著（整本书或书中某一章节）(Book)
Gregersen H, Penzien J, 2006. Biomechanics of the Gastrointestinal Tract. 2nd Edition. People’s Medical Publishing House, Beijing, China, p.216-236 (in Chinese).
Prigogine I, 1976. Order through fluctuation: self-organization and social system. In: Jantsch E, Waddington C (Eds.), Evolution and Consciousness: Human Systems in Transition. Addison-Wesley, London, UK, p.93-134.

学位论文(Thesis)
Rizvi UH, 2006. Combined Multiple Transmit Antennas and Multi-level Modulation Techniques. PhD Thesis, Royal Institute of Technology, Stockholm, Sweden.

科技报告(Report)
Sweeney L, 2000. Uniqueness of Simple Demographics in the U.S. Population. Technical Report No. LIDAP-WP4, Laboratory for International Data Privacy, Carnegie Mellon University, Pittsburgh, USA.
标准(Standard)
ISO (International Organization for Standardization), 1982. Steels-Classification-Part 1: Classification of Steels into Unalloyed and Alloy Steels Based on Chemical Composition, ISO 4948-1:1982. ISO, Geneva, Switzerland.

SEPA (State Environmental Protection Administration), 1997. Integrated Emission Standard of Air Pollutants, GB 16297-1996. National Standards of the People’s Republic of China. 
专利(Patent)
Cookson AH, 1985. Particle Trap for Compressed Gas Insulated Transmission Systems. US Patent 4554399.
网页(Webpage)
University of Sheffield Library, 2001. Citing Electronic Sources of Information. University of Sheffield.

http://www.shef.ac.uk/library/libdocs/hsl-dvc1.pdf
正文引用格式(Citation format)
文献只有一个作者(one author)：
(Vandermeer, 1990)
Vandermeer (1990)
文献有两个作者(two authors)：
(Sun and Wang, 2000)
Cao and Xu (2001)
文献有三个或以上作者(three or more authors)：
(Moons et al., 1997; Schlag et al., 2001a, 2001b)

Schlag et al. (2001a, 2001b)

[image: image19.png]






( Sisi LI, xxxxx@zju.edu.cn


� San ZHANG, https://orcid.org/0000-0000-0000-0001


Sisi LI, https://orcid.org/0000-0000-0000-0002





Received Jan. xx, 2026; Revision accepted Apr. xx, 2026; 


Crosschecked 





© Zhejiang University Press 2026








_1491206408.unknown

_1491998600.unknown

_1703425667.vsd
�

Fx



_1708870838.unknown

_1491999420.unknown

_1491682584.unknown

_1490168052.unknown

_1490301094.unknown

_1490301204.unknown

_1490168031.unknown

